## Slide 1
future materials…
… made by today’s people
Advanced Materials for Energy Applications
Innovative and Sustainable Polymeric Materials
Cells for Materials and Materials for Cells
Multifunctional Surfaces
Life Cycle Thinking
Characterization Platform
©MateriaNova

## Slide 2
Sol-gel encapsulation of microorganism:
coating characterization and enzyme activity determination
Tangi Senechal
C. Castro, D. Lahem, A-L. Hantson
Amsterdam, 27/06/2018
Notes: 2

## Slide 3
Presentation of the study
Sol-gel and microorganism preparation
Enzymatic activity testing
Experimental design
Enzyme activity results
Alternative enzyme activity testing

## Slide 4
BIODEC project aim to reduce indoor air pollutant
SUBSTRAT
SUBSTRAT
Incorporation of Pseudomonas putida
Expressing Formaldehyde deshydrogenase
In Dev.

## Slide 5
Coating formulations
sol-gel coating
  Mechanical properties
  Control of the hydrophobicity
  Chemical resistance
  Durability
Enzymes viability
  Low temperature
  No alcohol
  No extreme pH
  No UV
  No Ultrasound
Coatings containing Pleurotus ostreatus as a control microorganism,
following enzyme viability through laccase activity

## Slide 6
sol-gel coating
Metalloid (Si, Ti, Zr…)
+ hydrolysable groups (alkoxyde, OR)
Dip-coating
Coating formulations

## Slide 7
sol-gel coating - precursors
TEOS
GPTMS
PVOH
PEG
Coating formulations
With water and acetic acid

## Slide 8
sol-gel coating - precursors
Coating formulations
Addition of PVOH to the formulation :
Room temperature reticulation
(50 MEK cycles)
Wettability : water contact angle
(from 80 ° without to 60 ° with PVOH)

## Slide 9
Micro-organism preparation
Homogeneization
grinding
Freeze drying
Pleurotus ostreatus
* Dead microorganism with active enzymes
* Water dispersible

## Slide 10
Coating formulations for enzyme viability
Hydrolysis and condensation
Addition of freeze-dried
microorganism
TEOS GPTMS PVOH
Ethanol removal
Phosphate buffer
pH 2,5  ~5
Dip coating
Room temperature reticulation
M. L. Ferrer, L. Yuste, F. Rojo and F. del Monte, Chem. Mater., 2003, 15, 3614–3618.

## Slide 11
Enzymatic activity testing
Pleurotus ostreatus expresses laccase enzyme for lignase activity
Laccase activity is followed by a redox mediator – ABTS
ABTS is oxidized to cationic state, responsible of blue-green color
    Kinetics of extinction of ABTS+ at 420 nm
175 µL ABTS + 50 µL sample + 775 µL buffer carbonate-tartrate  Laccase activity

## Slide 12
Enzymatic activity testing
1 formulation
3 microorganism ratios
20 %
30 %
40 %
3 deposition speed
100 mm/min
250 mm/min
400 mm/min
Globally low absorbance
increase of the thickness with the withdrawal speed  Increase of the absorbtion
Landau-levich equation
    h = coating thickness
    η = viscosity
    γLV = liquid-vapour surface tension
    ρ = density
    g = gravity

## Slide 13
Enzymatic activity testing
Better microorganism dispersion
1 vs 3 layers of coating
2 deposition speed
100 mm/min
400 mm/min
Higher enzyme activity (abs and time)
Influence of layer and speed  thickness
    When speed increase– increase of thickness by 38%
    When 3 layers  increase of thickness by 236%

## Slide 14
Experimental design
Modification of coating parameters :
Precursor ratio TEOS/GPTMS 1/0,1 – 1/0,3 – 1/0,5
Addition of PEG 600 0 – 2,5 % - 5 % molar/TEOS
Microorganism ratio 20 % - 30 % - 40 % mass/sol-gel
Speed of deposition 200 – 400 – 600 mm/min

## Slide 15
Experimental design
Optimized Experimental Design (OED)
4 factors
3 levels for each factor
1 central point
2 Replicates
5 samples for each condition
TEOS/GTMS 1/0.1 formulations tends to a quick gelation

## Slide 16
Experimental design
Dip coating on cover glass
5 samples for each condition
Coated covers in contact with ABTS solution
well plate
Automatic spectroscopy testin using
SYNERGY H1M from Biotek

## Slide 17
Enzyme activity results
Quick look at the results:
Higher absorbance for  higher µorganism ratio
           higher PEG ratio
           higher speed of deposition
Precursor ratio does not seem the most impactant

## Slide 18
Enzyme activity results
Stastistical analysis of the OED
Extended estimation |  |  |  | 
Error |  |  |  | 
 | Estimation | Standard | T ratio | Prob. > ¦t¦
Constant | 0,2389 | 0,0517 | 4,62 | 0,0007
Precursor | 0,0475 | 0,0574 | 0,83 | 0,4261
PEG | 0,1247 | 0,0574 | 2,17 | 0,0527
Microorganism | 0,1567 | 0,0574 | 2,73 | 0,0196
Withdrawal speed | 5,65E-5 | 0,0574 | 0,00 | 0,9992
Statistical analysis (main conclusions):
The concentration of microorganism in the coating significantly increases laccase activity (p-value < 0.05)
Laccase activity also increases with the increase of PEG concentration

## Slide 19
Enzyme activity results
Combination of factors
Combination of high PEG and microorganism ratio lead to the highest enzyme activity
Precursor ratio and withdrawal speed have the lowest impact on laccase activity

## Slide 20
Direct detection with colorants
Preliminary results:
Coatings tested: latex, TEOS+GPTMS; TEOS+GPTMS+PVOH
Need of atmospheric humidity to avoid coatings drying over time (decrease of the microbiological activity on the surface of the supports)
Not possible to detect laccase activity using this methodology either using the glass blades or the glass beads
Hermetic cage:
relative humidity ≈ 80 %
Objective : Detection of enzyme activity directly on the coated substrate
Alternative enzyme activity testing

## Slide 21
Direct detection of laccase activity
Time evolution of the selected colorants – glass blades
1
4
2
3
5
6
1 – Methyl red
2 – Phenol red
3 – Methyl thymol blue
4 - Methylene blue
5 – Methyl orange
6 - ABTS
Latex coating
Latex coating
+
P. ostreatus
Day 0
Day 1
Day 9
Day 10
Day 15
Phenol red and methyl orange changed in the presence of laccase
Alternative enzyme activity testing

## Slide 22
Direct detection of laccase activity
Time evolution of the selected colorants – glass beads
Methyl red
Day
0
Day
1
Day
9
Day
10
Day 15
Day
0
Day
1
Day
9
Day 10
Day 15
Phenol red
Methyl thymol blue
Methylene blue
Methyl orange
ABTS
Latex coating
Latex coating + P. ostreatus
Alternative enzyme activity testing
Methylene blue and methyl orange changed in the presence of laccase

## Slide 23
Conclusion and perspective
Sol-gel coating with active enzymes on microorganism
Analysis of enzyme activity of a coated substrates
Optimized experimental design to evaluate formulations and
coating parameters
Alternative reactants to be used directly on substrates
Replacement of the actual microorganism by one expressing FDH
Studying durability of the system (cofactor regeneration
– water availability) and coating mechanical properties
Monitoring the efficiency of the system (measurement of
formaldehyde degradation – sensors adapted)

## Slide 24
©MateriaNova
www.materianova.be
Thanks for your attention
tangi.senechal@materianova.be

## Slide 25
Thickness measurements:
Without microorganism
100 mm/min  3 µm
200 mm/min  5 µm
400 mm/min  12 µm
600 mm/min  14 µm
With 20 % microorganism
100 mm/min  37 µm
200 mm/min  42 µm
400 mm/min  70 µm
600 mm/min  80 µm