# Supporting Information

# NMR relaxometry to monitor in situ the loading of Amberlite IR120 and Dowex Marathon MSC resins with Ni2+ and Cu2+ during a column experiment

Marie Bernardia, Rodrigo De Oliveira-Silvab, Quoc Lam Vuonga, Dimitrios Sakellarioub, Yves Gossuina

aBiomedical Physics Unit, Research Institute for Materials Science and Engineering, UMONS, 25 avenue Maistriau, 7000 Mons, Belgium

bCentre for Membrane Separations, Adsorption, Catalysis and Spectroscopy (cMACS), KU Leuven, 200 F Box 2454 Celestijnenlaan, 3001 Leuven, Belgium

Corresponding author: Yves Gossuin, yves.gossuin@umons.ac.be

Figure S1: Evolution of the amplitude Afast of the fast fraction obtained by the biexponential fitting of the relaxation curves during a column experiment with IR120 resin and a 20 mM Ni2+ solution. mresin = 14 g, flow rate = 4.3 ml/min.

Figure S2: Evolution of the relaxation rate 1/T2,fast of the fast fraction obtained by the biexponential fitting of the relaxation curves during a column experiment with IR120 resin and a 20 mM Ni2+ solution. mresin = 14 g, flow rate = 4.3 ml/min.

Figure S3: Evolution with time of the amplitude Afast of the fast fraction obtained by the biexponential fitting of the relaxation curves during a column experiment with IR120 resin and a 20 mM Ni2+ solution, for three different heights of the studied zone of the resin bed. mresin = 14 g, flow rate = 4.3 ml/min.

Figure S4: Evolution with time of the relaxation rate 1/T2,fast of the fast fraction obtained by the biexponential fitting of the relaxation curves during a column experiment with IR120 resin and a 20 mM Ni2+ solution, for three different heights of the studied zone of the resin bed. mresin = 14 g, flow rate = 4.3 ml/min.

Figure S5: Curves of return to equilibrium of longitudinal magnetization for the bottom of the column bed a) before (t = 0 h), b) during (t = 2.2 h) and c) after (t = 4.7 h) the loading of IR120 resin with Ni2+ ions. mresin = 14 g, flow rate = 4.3 ml/min.

Figure S6: Loading of Marathon MSC resin with Ni2+ ions. T2 distribution obtained by the Inverse Laplace Transform of the CPMG relaxation curves. mresin = 12.3 g, flow rate = 4.3 ml/min.

Figure S7: curve of return to equilibrium of transverse magnetization for the bottom of the column bed after (t = 4.94 h) the complete loading of IR120 resin with Cu2+ ions.

Figure S8: Loading of IR120 resin with Cu2+ ions. T2 distribution obtained by the Inverse Laplace Transform of the CPMG relaxation curves. mresin = 14 g, flow rate = 4.3 ml/min.

Figure S9: Loading of Marathon MSC resin with Cu2+ ions. T2 distribution obtained by the Inverse Laplace Transform of the CPMG relaxation curves. mresin = 12.3 g, flow rate = 4.3 ml/min.