## Slide 1
NMRD analysis showed increased relaxivity in aqueous media, attributed to micelle-induced rotational restriction. Our compound offers enhanced contrast properties compared to its monomeric form in methanol.
Critical Micelle Concentration (CMC) was determined using a fluorescence-based method with Nile Red as a hydrophobic probe. The critical micelle concentration was calculated to be 0.20 mM, confirming the compound’s ability to self-assemble in aqueous media.
Dynamic Light Scattering (DLS) analysis of the radioswitch micelles in PBS at 25°C shows a hydrodynamic diameter of 11.1 nm (PDI: 5.96%).
Light-Responsive Azo-Micelles for Controlled Drug Release and MRI Monitoring
1Department of General, Organic and Biomedical Chemistry, NMR and Molecular Imaging Laboratory, University of Mons, 7000 Mons, Belgium
2CMMI – Center for Microscopy and Molecular Imaging, 6041 Gosselies, Belgium
Melisa Esther Gonzalez1, Thomas Vangijzegem1, Nathan Duchemin1, Dimitri Stanicki1 and Sophie Laurent1,2
INTRODUCTION
Current research on light-sensitive systems for drug delivery and imaging highlights the relevance of azobenzene-based compounds1. In this work, we present the synthesis of a radioswitch molecule based on 4-octyloxyazobenzene, functionalized with a PEG linker and complexed with Gd-DOTA. This compound forms micelles in aqueous media, undergoes stimuli-responsive isomerization upon UV exposure, and demonstrates MRI-relevant relaxivity, making it a promising candidate for dual-function imaging and controlled drug release applications.
Synthesis of Radioswitch Molecules
Micelle Formation Characterized by DLS
Light-Induced Isomerization
Thermal Back-Isomerization
NMRD Profile and Relaxivity Enhancement
Conclusion
Determination of CMC
Figure 1. Schematic representation of an Azo-DOTA compound comprising (i) an ionizing radiation (IR)-responsive Gd chelate (red), (ii) a light-sensitive azobenzene photoswitch (blue), and (iii) variable hydrophobic chains (green, R). The diagram also illustrates micelle self-assembly and its disruption upon UV or X-ray exposure via azobenzene isomerization, triggering drug release.
Azobenzene-(Gd)-DOTA compound underwent efficient trans-to-cis isomerization upon UV irradiation, monitored by UV–Vis spectroscopy.
After reaching the photostationary state (PSS), thermal back-isomerization at 37°C followed a one-phase exponential model, with a cis-isomer half-life of 29 minutes.
These results confirm the reversible and controllable behavior of the radioswitch.
Radioswitch molecule was successfully synthesized and characterized. It forms stable micelles in aqueous media, responds to light and ionizing radiation via reversible isomerization, and enhances MRI relaxivity.
These features support its potential as a dual-function system for stimuli-responsive drug delivery and MRI monitoring.
References: 1- A. Guesdon-Vennerie, P. Couvreur, F. Ali et al. Nat Commun, 2022, 13, 4102.
Acknowledgments: this work was performed with the financial support of the F.R.S.-FNRS – Télévie.
MelisaEsther.GONZALEZ@umons.ac.be
RESULTS