## Slide 1
Impact of Hybrid Nanoparticle Aggregation on Optical Response, Heat Generation, and MRI Contrast
C. Rousseau1 , Q.L. Vuong2, Y. Gossuin2, B. Maes1 and G. Rosolen1
1 Micro- and Nanophotonic Materials Group, Research Institute for Materials Science and Engineering, University of Mons
2 Biomedical Physics Unit, University of Mons
Notes: Les propriétés optiques de quelques couches d'InSe

## Slide 2
Treatment phase: Phototermal therapy (PTT)
Diagnostic phase: Magnetic Resonance Imaging (MRI)
Contrast agents
Photothermal agents
NIR Laser
What is the research context?

## Slide 3
Theranostic approach: MRI + PTT
?
Contrast/Photothermal
agents
Underlying question:
“How will the use of phototherapy modify MRI images?”
NIR Laser
What is the research context?

## Slide 4
More precise question:
“How does laser illumination of a solution
modify its transverse relaxation rate (R2)? ”
What is the research context?
Theranostic approach: MRI + PTT
?
Contrast/Photothermal
agents
NIR Laser
Underlying question:
“How will the use of phototherapy modify MRI images?”

## Slide 5
Magnetite core (Fe3O4): allow MRI
Plasmonic hybridization between nanosphere/nanocavity
magnetite core radius: 150 nm
gold shell thickness: 20 nm
Biological window
Gold nanoshell: allow PTT ≈ + 6°C
Hybrid nanoshell platforms are effective tunable Contrast/Photothermal agents

## Slide 6
Optimization of nanoshell geometry
10 nm shell → higher absorption for a large gamme a radius core
Increasing core radius
Dipolar peaks
Quadrupolar peaks

## Slide 7
Best absorption peak chosen in the biological window
Optimization of nanoshell geometry

## Slide 8
Therapeutic laser irradiance
= 1 W/cm2
High laser irradiance
= 10000 W/cm2
magnetite core radius: 55 nm
gold shell thickness: 10 nm
Is the therapeutic irradiance not enough for phototherapy?

## Slide 9
Collective thermal effects lead to a significant increase in temperature
Laser beam
Absorption cross section
Extinction cross section
Distance in sample
Water absorption coefficient
NPs concentration

## Slide 10
Collective thermal effects lead to a significant increase in temperature
Sufficient temperature elevation for photothermal therapy

## Slide 11
Sample without
magnetic field
Constant magnetic
field
Oscillating magnetic
field
Relaxation
Resulting magnetization
System out of equilibrium
Return to magnetization equilibrium
Randomized magnetic moments
MRI imaging based on the relaxation
( described by a relaxation rate)
Nuclear magnetic resonance in 4 steps

## Slide 12
Influence on relaxation: nanoparticle size and medium temperature
Increasing size
Medium
temperature ↗

## Slide 13
Calculation procedure of the relaxation maps
Calculation of the temperature elevation map
Voxel discretization procedure
Choice of the relaxation model for each voxel

## Slide 14
Relaxation maps due to laser illumination
Magnetite core : 20 nm
Gold shell : 10 nm
Magnetite core : 95 nm
Gold shell : 10 nm
Magnetite core : 150 nm
Gold shell : 10 nm
Up to 30% modification for a core radius around 20-25 nm !

## Slide 15
Two different types of aggregation
Michael Levy et al., Biomaterials 2011
Jinxing Chen et al, ACS Nano 2022
Natural aggregation
Designed aggregation
Is there an optimal degree of aggregation?

## Slide 16
Studied nanoshell clusters
Minimum approach distance = 1 nm
Magnetite core : 20 nm
Gold shell : 10 nm

## Slide 17
Adjustment of aggregation through cluster stretching
Studied nanoshell clusters
Magnetite core : 20 nm
Gold shell : 10 nm

## Slide 18
Calculation of the average temperature rise on the surface of the cluster
Studied nanoshell clusters
Magnetite core : 20 nm
Gold shell : 10 nm

## Slide 19
Optimal volume fraction to achieve a maximum temperature increase
20 x
150 x
300 x
The optimum position depends on the number
of NPs in the cluster

## Slide 20
Optimal volume fraction to achieve a maximum temperature increase
Possibility of deriving a law to calculate the optimal radius of a cluster of N particles

## Slide 21
Cluster solution: mean optical and thermal response
+
+
+…
+
+
Biological window
Link with average absorption cross-section
Possibility to use the collective model for cluster solutions
50 x

## Slide 22
50 x
100 x
500 x
Tracking the separation of clusters by MRI?
Ambiant relaxation rate ≈ laser focus relaxation rate

## Slide 23
50 x
100 x
500 x
Tracking the separation of clusters by MRI?
Up to 50% modification when dividing the number of NPs by 10!
R2 = 80
R2 = 64
R2 = 35

## Slide 24
Conclusion
Optimal Ns geometry
20-25 nm radius core
10 nm thickness shell
Highlighting the potential for tracking cluster separation by MRI
Framework for mapping changes in R2
due to phototherapy
with Ns
Outlook
Adaptation of the framework to handle regions with different concentration levels
Consider a high scattering medium to mimic human tissues
VS