## Slide 1: Effect of EAF slag basicity on steel-slag equilibrium and chromium oxidation
valentin.nitelet@umons.ac.be
Valentin Nitelet1, Hoang Tran², Alessandro D'Alfonso³, Jean-Christophe Pierret², Alexandre Mégret1, Véronique Vitry1
1 Metallurgy Department, Faculty of Engineering, UMONS-University of Mons, Belgium
2 Center for Research in Metallurgy (CRM), Liège, Belgium
³ APERAM, Charleroi, Belgium

## Slide 2: Context
Valentin Nitelet
PhD student at the Faculty of Engineering at the University of Mons in Belgium
Stainless steelmaking
Electric arc furnace (EAF) route
Evolution to increase efficiency and productivity
Decreasing time
Numerical model for stainless steel
Context/EAF Process/Method/Steel-Slag equilibrium/Comparison FactSage/Chromium oxidation/Conclusion
Better knowledge of the process
Recycling(1)
CO2 production(2)
(1) J. Muract, “MAN01052 – Electric Arc Furnace - steeluniversity,” Jul. 2016. [Online]. Available: https://steeluniversity.org/courses/man01052-electric-arc-furnace/
(2) S. Jahanshahi, J. G. Mathieson, M. A. Somerville, N. Haque, T. E. Norgate, A. Deev, Y. Pan, D. Xie, P. Ridgeway, and P. Zulli, “Development of Low-Emission Integrated Steelmaking Process,” Journal of Sustainable Metallurgy, vol. 1, no. 1, pp. 94–114, Mar. 2015. [Online]. Available: https://doi.org/10.1007/s40831-015-0008-6

## Slide 3: Context
Thermodynamic considerations
Expression of K for many reactions
Carbon steel
Stainless steel
New expression of K for the reactions
Calculation Phase Diagram modelling (CalPhaD)
Thermo-Calc
High concentration (>11wt.% of Cr)
Reactions
Reactions
Context/EAF Process/Method/Steel-Slag equilibrium/Comparison FactSage/Chromium oxidation/Conclusion
Adaptation of a model on the EAF process for stainless steel
CRM Model
CRM: Center
of Research
in Metallurgy (Be)

## Slide 4: Electric Arc Furnace (EAF) Process(1)
Furnace
Roof
Wall in refractory materials (e.g. MgO for stainless steel)
Water cooling system
Steel
Burners and oxygen injection
Electrodes
Context/EAF Process/Method/Steel-Slag equilibrium/Comparison FactSage/Chromium oxidation/Conclusion
(1) J. Muract, “MAN01052 – Electric Arc Furnace - steeluniversity,” Jul. 2016. [Online]. Available: https://steeluniversity.org/courses/man01052-electric-arc-furnace/

## Slide 5: Electric Arc Furnace (EAF) Process(1)
To be continued…
Basket preparation:
2/3 baskets with scraps
Melt down charging 1
Charging of basket 2
Melt down charging 2
Refining
Tapping
Charging of basket 1
Chart: 
| 0 | 1 | 2 | 3 | 4 | 5 | 5 | 6 | 6 | 10 | 10 | 15 | 18.5 | 18.5 | 19.5 | 19.5 | 23.5 | 23.5 | 28 | 28 | 31
 | 0 | 0 | 0 | 0 | 0 | 0 | 0.5 | 0.5 | 1 | 1 | 0 | 0 | 0 | 0.5 | 0.5 | 1 | 1 | 0.75 | 0.75 | 0 | 0
Power supply during the process
Addition of oxide and injection of oxygen and natural gas
Addition of oxide and injection of oxygen and natural gas
Addition of oxide and injection of oxygen
Context/EAF Process/Method/Steel-Slag equilibrium/Comparison FactSage/Chromium oxidation/Conclusion
(1) J. Muract, “MAN01052 – Electric Arc Furnace - steeluniversity,” Jul. 2016. [Online]. Available: https://steeluniversity.org/courses/man01052-electric-arc-furnace/

## Slide 6: Electric Arc Furnace (EAF) Process(1)
Slag = mix of oxides
Important Property of the slag for these purposes
Basic | 
Acid | 
Amphoteric | 
Basic | 
Acid | 
Amphoteric | 
To protect the refractory on the wall
To help for refining step
To protect steel thermally
from the outside
Study the influence of slag basicity on equilibrium steel-slag
Slag
Steel
Context/EAF Process/Method/Steel-Slag equilibrium/Comparison FactSage/Chromium oxidation/Conclusion
(1) J. Muract, “MAN01052 – Electric Arc Furnace - steeluniversity,” Jul. 2016. [Online]. Available: https://steeluniversity.org/courses/man01052-electric-arc-furnace/

## Slide 7: Method
Stainless Steel
0.1
0.5
1
1.5
2
0 wt.%
10 wt.%
20 wt.%
304 grade
Oxygen
Fe | 71.18
Cr | 18
C | 0.07
Ni | 8
Si | 0.75
Mn | 2
Steel composition
[wt.%]
Context/EAF Process/Method/Steel-Slag equilibrium/Comparison FactSage/Chromium oxidation/Conclusion
Basicity
System
Slag
Amount of FeO

## Slide 8: Method
Composition [wt.%] | 10 wt.% FeO |  |  |  | 
 | 71.8 | 53 | 40 | 32 | 26
 | 11 |  |  |  | 
 | 7.2 | 26 | 39 | 47 | 53
Basicity | 0.1 | 0.5 | 1 | 1.5 | 2
Composition [wt.%] | 10 wt.% FeO |  |  |  | 
 | 71.8 | 53 | 40 | 32 | 26
 | 11 |  |  |  | 
 | 7.2 | 26 | 39 | 47 | 53
Basicity | 0.1 | 0.5 | 1 | 1.5 | 2
Composition [wt.%] | 20 wt.% FeO |  |  |  | 
 | 62.7 | 46 | 34.5 | 27.6 | 23
 | 11 |  |  |  | 
 | 6.3 | 23 | 34.5 | 41.4 | 46
Basicity | 0.1 | 0.5 | 1 | 1.5 | 2
Composition [wt.%] | 20 wt.% FeO |  |  |  | 
 | 62.7 | 46 | 34.5 | 27.6 | 23
 | 11 |  |  |  | 
 | 6.3 | 23 | 34.5 | 41.4 | 46
Basicity | 0.1 | 0.5 | 1 | 1.5 | 2
Composition [wt.%] | 0 wt.% FeO |  |  |  | 
 | 80.9 | 59 | 45 | 36 | 30
 | 11 |  |  |  | 
 | 8.1 | 30 | 44 | 53 | 59
Basicity | 0.1 | 0.5 | 1 | 1.5 | 2
Composition [wt.%] | 0 wt.% FeO |  |  |  | 
 | 80.9 | 59 | 45 | 36 | 30
 | 11 |  |  |  | 
 | 8.1 | 30 | 44 | 53 | 59
Basicity | 0.1 | 0.5 | 1 | 1.5 | 2
Context/EAF Process/Method/Steel-Slag equilibrium/Comparison FactSage/Chromium oxidation/Conclusion

## Slide 9: Steel-Slag equilibrium
Context/EAF Process/Method/Steel-Slag equilibrium/Comparison FactSage/Chromium oxidation/Conclusion

## Slide 10: Steel-Slag equilibrium
Reactions | 0 wt.% FeO | 10 wt.% FeO | 20 wt.% FeO
Reactions | 0 wt.% FeO | 10 wt.% FeO | 20 wt.% FeO
The trend line depends on the dataset
Is the difference significant?
The step of Thermo-Calc
Not significant
More steps at the beginning
Context/EAF Process/Method/Steel-Slag equilibrium/Comparison FactSage/Chromium oxidation/Conclusion
More steps at the end
Temperature step can change during the simulation

## Slide 11: Comparison with FactSage
Where does the difference come from?
Database?
Research to determine whether the difference is significant
Context/EAF Process/Method/Steel-Slag equilibrium/Comparison FactSage/Chromium oxidation/Conclusion
FactSage Basicity 2
Thermo-Calc Basicity 2
Relatively similar

## Slide 12: Conclusion on the expressions
What is the next step?
We have the expressions of Log(K) as a function of the temperature
To wait for the industrial trials
Nothing else?
Let’s talk about another aspect of stainless steel
Context/EAF Process/Method/Steel-Slag equilibrium/Comparison FactSage/Chromium oxidation/Conclusion

## Slide 13
Steel with at least 11 wt.% of chromium
Stainless steel
Injection of oxygen at the EAF process
Oxidation of chromium before oxidation of carbon(1)
We want to decrease the loss of chromium and increase the reduction of chromium oxide
Chromium oxide goes in the slag
Unwanted
To reduce the chromium oxide from the slag to the Stainless Steel(2)
=
Recovery step
FeSi
Basicity effect on the activity of chromium and chromium oxide
Context/EAF Process/Method/Steel-Slag equilibrium/Comparison/Chromium oxidation/Conclusion
Ma, Z. and Janke, D. (2003), Thermodynamic Assessment to Chromium Oxidation in the Production of Stainless Steel. steel research international, 74: 99-103. https://doi.org/10.1002/srin.200300167
Guo, M., Durinck, D., Jones, P.T., Heylen, G., Hendrickx, R., Baeten, R., Blanpain, B. and Wollants, P. (2007), EAF Stainless Steel Refining - Part I: Observational Study on Chromium Recovery in an Eccentric Bottom Tapping Furnace and a Spout Tapping Furnace. steel research international, 78: 117-124. https://doi.org/10.1002/srin.200705868

## Slide 14
The condition are desired to decrease the chromium oxidation
To decrease the activity of chromium(1)
The conditions are desired to increase the chromium oxide reduction
To increase the chromium oxide activity(2)
The choice of the reducing agent(2)
Basicity
Context/EAF Process/Method/Steel-Slag equilibrium/Comparison FactSage/Chromium oxidation/Conclusion
Basicity effect on the activity of chromium and chromium oxide
Ma, Z. and Janke, D. (2003), Thermodynamic Assessment to Chromium Oxidation in the Production of Stainless Steel. steel research international, 74: 99-103. https://doi.org/10.1002/srin.200300167
Guo, M., Durinck, D., Jones, P.T., Heylen, G., Hendrickx, R., Baeten, R., Blanpain, B. and Wollants, P. (2007), EAF Stainless Steel Refining - Part I: Observational Study on Chromium Recovery in an Eccentric Bottom Tapping Furnace and a Spout Tapping Furnace. steel research international, 78: 117-124. https://doi.org/10.1002/srin.200705868

## Slide 16: Basicity effect on the activity of chromium and chromium oxide
To decrease the activity of chromium
To increase the activity of chromium oxide
BASICITY
Purposes of the slag
Protect the refractory on the wall
Help for refining step
Protect steel thermally from outside
Usually refactory wall: based on MgO
  Slag saturated in MgO (~11wt.% MgO) Basic oxide
  Slag with a higher basicity to protect the wall
  Basicity needs to balance the production of
BASICITY around ~1-1.5
Context/EAF Process/Method/Steel-Slag equilibrium/Comparison FactSage/Chromium oxidation/Conclusion
BASICITY

## Slide 17: Conclusion
Thank you
for your attention
Basicity effect on the activity of chromium and chromium oxide
Basicity has an effect on chromium and chromium oxide activities
Opposite effect  We need to optimise the condition
To study other reducing agents instead of FeSi
The influence of slag basicity on equilibrium steel-slag
Basicity affects elements and oxide activities
Very low effect of the slag basicity on the equilibrium constant
To consider other elements that could affect the equilibrium constant
To make the industrial trials to verify the expressions and validate the model
Context/EAF Process/Method/Steel-Slag equilibrium/Comparison FactSage/Chromium oxidation/Conclusion
I want to thank the Walloon region for the funding
(Convention: 8948), my co-supervisor, CRM, APERAM and Nicholas from Thermo-Calc