## Slide 1: Alcanivorax borkumensis, a key player for the low-density polyethylene degradation
Alice Delacuvellerie
Proteomics and Microbiology Laboratory University of Mons (Belgium)

## Slide 2
Introduction
5 trillions of plastic pieces into oceans
(Geyer et al., 2017)

## Slide 3
Introduction
(Rochman, 2015)
(Kühn et al., 2015)
© Delacuvellerie

## Slide 4
Introduction
1 µm
© Delacuvellerie Alice
Plastisphere
Understand their effects and roles in ecosystems
Understand their role in dispersal of pathogenic species
Study potential candidates for plastic degradation
New substrates
Dispersion vectors
Carbon sources
(Artham & Doble, 2008)

## Slide 5
Methods
Floating plastics (PFS)
Sediment plastics (PH)
Sediment (SSH)

## Slide 6
A. Delacuvellerie et al., Hazardous materials, 2019
Bacterial community structure
Richness
Equitability
Distinctness bacterial community from plastics and sediments
Plastic is a disctinct environmental niche

## Slide 7
A. Delacuvellerie et al., Hazardous materials, 2019
Bacterial community structure
Richness
Equitability
Floating plastics
Sediment plastics

## Slide 8
A. Delacuvellerie et al., Hazardous materials, 2019
Enrichment cultures
Strong selection of 2 bacteria on LDPE:
Alcanivorax borkumensis
Microbulbifer sp.
LDPE
PET
PS

## Slide 9
Richness
Equitability
Percentage of A. borkumensis
Enrichment cultures
1 µm

## Slide 10
Hexadecane
LDPE
Isolation of Alcanivorax borkumensis

## Slide 11
Hexadecane
Biofilm formation by Alcanivorax borkumensis
LDPE
PS
LDPE
A. borkumensis clearly displayed a higher affinity for the LDPE (more than 70% of bacteria in biofilm) than the others

## Slide 12
LDPE degradation by Alcanivorax borkumensis
ATR-FTIR spectra revealed the formation of C=O and OOH/OH functional groups resulting from the polymer degradation

## Slide 13
Conclusion
Selection of Alcanivorax borkumensis on LDPE
Signs of degradation
Finding optimal condition to improve the LDPE degradation
Study of the mechanism of A. borkumensis for the LDPE degradation

## Slide 14
Acknowledgments
Supervisor: Prof. Ruddy Wattiez
Proteomics and Microbiology Laboratory:
Polymer and Composite Materials Laboratory: Samira Benali
Oceanology Department: Sylvie Gobert
National Scientific Research Fund (F.R.S-FNRS)